METHODOLOGY AND RESULTS-DISCUSSION DRAFT

Hybrid Degradation-Aware, Energy-Constrained Charging Optimization Using a Transfer-Learned Battery Digital Twin

Working research draft | 24 July 2026

Purpose: This editable draft consolidates the current physical modelling rationale, completed results, implementation priorities, and two prompts for efficient follow-up work. Replace bracketed placeholders only after the corresponding experiment is run.

# Scope and evidence status

The completed work consists of a transfer-learned battery digital twin, energy-constrained charging simulation, and profile optimization. Earlier results used a temperature-time reward with random search. The current implementation introduces a hybrid calendar-cyclic capacity-loss objective and GP Bayesian optimization. Reinforcement learning is a planned next stage and must not be described as a completed experimental result until trained and evaluated under the same constraints.

Scientific caution: The semi-empirical aging coefficients are drawn from literature sources with chemistry- and test-specific conditions. Until calibrated to the NASA RW cells, the reported Q_loss values should be called a relative capacity-loss index rather than an absolute percentage of capacity fade.

# 1. Research objective and hypotheses

The objective is to determine a feasible charging-current trajectory that delivers a specified energy requirement within an available charging interval while minimizing modelled calendar and cycling degradation. The battery state is propagated through a transfer-learned digital twin and a Coulomb-counted SoC state update.

H1: Under a fixed energy requirement and identical safety limits, the hybrid objective selects profiles with a more interpretable time-versus-degradation trade-off than the earlier temperature-time reward.

H2: At limited evaluation budgets, GP Bayesian optimization reaches lower feasible loss than random search for at least some profile families, particularly pulsed charging with higher-dimensional parameters.

H3: The preferred profile changes with initial SoC, required energy, available time, ambient temperature, and cell age; therefore a single lifetime profile is not sufficient for daily-use charging decisions.

# 2. Methodology

## 2.1 Battery digital twin and state propagation

A Transformer-decoder battery digital twin predicts terminal voltage V(t) and cell temperature T(t) from relative age, initial voltage, initial temperature, and the commanded charging-current sequence. The source model is trained on RW9 and fine-tuned on RW10-RW12. State of charge is not inferred from loaded terminal voltage; instead, it is updated through Coulomb counting using the age-dependent rated capacity and an OCV-SoC initialization.

## 2.2 Energy-constrained charging problem

For each charging session, the energy constraint is E_delivered >= E_required. E_delivered is obtained by integrating -V(t) I(t) over time. The decision variables are the parameters of CCCV, two-step, three-step, and pulsed charging families. Feasibility requires the energy target (or SoC target, where used) to be met within the maximum duration while respecting voltage and current limits.

## 2.3 Hybrid degradation model

The hybrid model separates calendar and cyclic stress rather than treating temperature only as a shaped reward. The total relative capacity-loss index is Q_loss,total = Q_calendar + Q_cyclic. The primary calendar model is the SoC-temperature-time Arrhenius relation (Eq. 2 in Sinha et al.). The primary cyclic model is the throughput-temperature-C-rate power-law relation (Eq. 7 and Table 7).

| Literature relation | Physical stress represented | Use in this work |
| --- | --- | --- |
| Eq. 2 | Calendar loss: mean SoC, T, time; Arrhenius dependence | Primary Q_calendar model |
| Eq. 3 | Alternative empirical calendar model | Sensitivity analysis; do not add to Eq. 2 |
| Eq. 4 | Equivalent full cycles, mean SoC and SoC swing | Report EFC, mean SoC and DeltaSoC; future stress multiplier |
| Eq. 5 | Temperature-time calendar loss | Alternative calendar sensitivity model |
| Eq. 6 | Generic Arrhenius aging rate | Physical rationale, not a separate additive loss |
| Eq. 7 / Table 7 | C-rate, T and Ah-throughput cyclic loss | Primary Q_cyclic model |
| Eq. 8 | Continuous current-dependent cyclic model | Future alternative after chemistry-specific calibration |

Model rule: Equations 2, 3 and 5 are alternatives for calendar aging. Equations 7/Table 7 and 8 are alternatives for cyclic aging. They should not be summed together without an experimentally justified coupling model.

## 2.4 Optimization objective

The session reward balances useful charge delivery, modelled degradation, and time: R = w_soc DeltaSoC - w_qloss(Q_calendar + Q_cyclic) - w_time t_h^z. The scalar loss is -R plus soft penalties for energy/SoC shortfall and voltage overshoot. For physical reporting, reward is secondary; energy, C-rate, temperature and each degradation component are reported separately.

## 2.5 Optimization and comparison protocol

Each family is optimized independently by Gaussian-process Bayesian optimization (PI acquisition in the completed RW9 experiments) and compared with random search under the same start state, energy/SoC requirement, current bounds, voltage ceiling, maximum duration, objective weights, and evaluation budget. A fair comparison evaluates the best feasible candidate rather than merely the best unconstrained score.

# 3. Results and discussion

## 3.1 Transfer-learning evidence

The two-stage fine-tuning procedure improves target-cell voltage prediction as more target-cell adaptation data are used. At 60% adaptation data, held-out voltage RMSE was 0.0323 V for RW10, 0.0483 V for RW11, and 0.0639 V for RW12. These results support use of target-specific twins for charging optimization, while the larger RW12 error motivates caution in extrapolating profile rankings across cells.

RW10, 60% adaptation: voltage RMSE = 0.0323 V; temperature RMSE = 0.2842 deg C.

RW11, 60% adaptation: voltage RMSE = 0.0483 V; temperature RMSE = 0.1517 deg C.

RW12, 60% adaptation: voltage RMSE = 0.0639 V; temperature RMSE = 0.2636 deg C.

## 3.2 Hybrid-objective GP-BO versus random search on RW9

For the completed RW9 comparison, the start state was SoC 20%, target SoC 80%, T0 = 24 deg C, age = 0, and the maximum duration was 150 min. At 40 evaluations per profile family, GP-BO selected a feasible pulsed profile with loss -0.3516, total reward 0.4121, duration 60.5 min, and relative total loss index 0.0937. The best random-search result was a three-step profile with loss -0.3450. Thus, GP-BO gave the best overall feasible solution at the limited 40-evaluation budget, while the family-level results show that the current three-step GP configuration remains a meaningful optimization limitation.

| Method / family | Budget | Best loss | Duration (min) | Q_loss index | Interpretation |
| --- | --- | --- | --- | --- | --- |
| GP-BO / pulsed | 40 | -0.3516 | 60.5 | 0.0937 | Best overall feasible result |
| Random / 3-step | 40 | -0.3450 | 63.0 | 0.0929 | Strong random baseline |
| GP-BO / pulsed | 80 | -0.3454 | 63.5 | 0.0936 | Near-tie at higher budget |
| Random / CCCV | 80 | -0.3452 | 63.5 | 0.0923 | Near-tie at higher budget |

Discussion: the 40-evaluation result supports sample efficiency for GP-BO in the pulsed family. It does not establish universal BO superiority: random search outperformed the current GP setup for three-step charging, and the 80-evaluation overall difference was negligible. This should be presented as an optimizer-behaviour finding, not hidden.

## 3.3 Physical interpretation of the hybrid objective

In the present single-session runs, Q_cyclic dominates Q_calendar because calendar aging depends on a much longer time scale. Accordingly, the hybrid ranking mainly reflects the compromise between charge time and cycling stress. A fast pulsed profile can rank first even with a slightly higher cyclic-loss index, because the time term is lower. This is a property of the stated weights, not evidence that pulsing universally extends battery life.

Interpretation boundary: Do not claim lithium plating, SEI thickness, resistance growth, LLI, or LAM has been directly measured. The current model uses stress-informed semi-empirical capacity-loss relations. High SoC, low temperature and high C-rate may be presented only as plating-risk proxies unless a negative-electrode-potential or validated electrochemical model is added.

## 3.4 Required figures for the supervisory review

| Figure | Axes / variables | Physical question answered |
| --- | --- | --- |
| Calendar-loss contour | mean SoC x T, colour Q_calendar | How SoC and temperature jointly accelerate calendar aging |
| Cyclic-loss curves | Ah throughput x Q_cyclic; C/2, 2C, 6C, 10C | How the Eq. 7/Table 7 model responds to C-rate |
| Cumulative degradation trajectory | time; I, V, T, SoC, cumulative Q_calendar and Q_cyclic | When each profile accumulates stress during charging |
| Equal-energy profile table | time, peak T, mean C-rate, Ah, Qcal, Qcyc | Which physical trade-off determines the selected family |
| Ambient sensitivity | 15, 25, 35 deg C; time, Tpeak, Qcal, Qcyc | Whether the selected strategy changes under thermal stress |
| Thermal cross-check | BDT Tpeak versus lumped-model Tpeak | Magnitude of thermal-model disagreement |

# 4. Implementation plan before Tuesday

Audit the equations and units. Confirm that the primary run uses Eq. 2 for calendar loss and Eq. 7/Table 7 for cyclic loss. Record coefficient source, chemistry, temperature unit, time unit, Ah unit, and whether Q_loss is normalized.

Add EFC, mean SoC and DeltaSoC to every profile report. These are needed to connect the energy-constrained session to Eq. 4 and depth-of-discharge stress.

Generate the six physical figures listed in Section 3.4 from the same fixed scenario. Do not change energy targets or constraints across compared profiles.

Run one reproducible RW9 hybrid comparison: GP-BO and random search, same seed and 40 evaluations per family. Preserve JSON, figure, command line, and Git commit in a run manifest.

Run an ambient sweep at 15, 25 and 35 deg C for at least CCCV, two-step and pulsed profiles. Report Q_calendar and Q_cyclic separately.

Implement a structured research dashboard only after the model report is stable. Inputs are numeric fields/dropdowns; no natural-language model is required.

Create the RL environment after the hybrid step reward has been verified. Do not present trained RL performance until it is compared with the same BO and CC baselines.

# 5. Structured daily-use interface specification

The interface should be a reproducible experiment and decision dashboard, not a natural-language assistant. It converts explicit user/system inputs into a constrained charging request. The interface does not itself establish novelty; the research contribution is the goal-conditioned, degradation-aware controller beneath it.

| Input | Unit / control | Physical role |
| --- | --- | --- |
| Cell ID / chemistry | dropdown | Selects capacity, OCV, voltage and current limits |
| Initial SoC | % | Initial lithium inventory / energy state |
| Initial and ambient temperature | deg C | Electro-thermal state and aging stress |
| Relative age / SoH | 0-1 or % | Capacity and resistance state |
| Required energy | Wh or pack-energy fraction | Hard service requirement |
| Available charging time | min | Deadline constraint |
| Charger current limit | A | C-rate and power bound |
| Maximum cell temperature | deg C | Thermal safety limit |
| Objective mode | fastest / balanced / minimum loss | Selects documented reward weights |

The outputs should be the top three feasible profiles, each with a current schedule, delivered energy, completion time, peak voltage, peak temperature, average C-rate, Ah throughput, Q_calendar, Q_cyclic, total loss index, and explicit constraint margins.

# 6. Phase prompts for future Codex use

Prompt 1 - Phase 1: physically interpretable hybrid degradation model

You are working in the battery_RW_NASA repository. Implement Phase 1: a physically interpretable hybrid degradation analysis for energy-constrained charging. Do not introduce an LLM or change unrelated code. First inspect Constrained_BO/hybrid_degradation.py, objective.py, simulator.py, run.py, and the existing RW9 result JSON files. Treat Eq. 2 (SoC-T-time Arrhenius) as the primary calendar model and Eq. 7/Table 7 (C-rate-T-Ah throughput) as the primary cyclic model. Eq. 3 and Eq. 5 must be selectable calendar sensitivity alternatives; Eq. 8 must be clearly marked as an alternative cyclic model unless its chemistry-specific coefficients are calibrated. Do not sum alternative equations. Add explicit model metadata and units to exported results; call the output a relative capacity-loss index unless a calibration establishes percent capacity fade. Add EFC, mean SoC, DeltaSoC, Ah throughput, mean/max C-rate, energy delivered/required, peak V, peak T, and constraint margins to per-profile metrics. Add deterministic tests for monotonic behavior: calendar loss increases with SoC/T/time; cyclic loss increases with Ah and C-rate under the selected model. Add a plotting/report script that generates: (1) Eq. 2 SoC-T contour, (2) Eq. 7/Table 7 Qcyc-vs-Ah curves at C/2, 2C, 6C, 10C, (3) cumulative Qcal/Qcyc along each best profile, and (4) equal-energy profile comparison table. Preserve backward compatibility, update README methodology wording, run the tests, and report exact files changed plus any limitations due to chemistry-specific coefficients.

Prompt 2 - Phase 2: safe goal-conditioned RL environment

You are working in the battery_RW_NASA repository. Implement Phase 2: a safe, goal-conditioned reinforcement-learning environment on top of the verified hybrid-degradation charging simulator. This is not a natural-language interface. Build a reproducible Python environment whose observation at each decision interval includes SoC, terminal voltage, cell temperature, relative age/SoH, previous current, remaining energy requirement, remaining time, ambient temperature, and optional uncertainty margin. Start with a discrete action set of safe charging-current levels; do not add deep-RL dependencies until the environment and tests work. Use the existing FrozenBDT/ChargingSimulator rollout and compute_step_reward so the per-step reward is incremental delivered energy minus Qcalendar increment, Qcyclic increment, and time increment. Enforce hard safety by action masking/projection before rollout: V <= Vmax, T <= Tmax, ¦I¦ <= Imax, and session must meet the remaining-energy/deadline requirement. Add a Gymnasium-compatible wrapper only if Gymnasium is already available; otherwise implement a small dependency-free environment with reset/step. Add deterministic tests for energy accounting, action rejection, reward decomposition, terminal conditions, and reproducibility. Provide baseline evaluation hooks for CCCV, the saved BO profile, and a simple tabular Q-learning agent. Save each episode with physical metrics (Wh, Ah, C-rate, Qcalendar, Qcyclic, peak V/T, feasibility), not just reward. Do not claim RL results until the agent is trained across multiple seeds and evaluated under exactly the same initial-state and energy/deadline scenarios as BO.

# 7. References used in this draft

Sinha, S. S., Lehman, B., and Bharadwaj, P. (2026). Life Extension of Lithium-Ion Battery: Degradation Comprehension, Modeling, Characterization, and Mitigation Strategies. IEEE Open Journal of Power Electronics, 7. DOI: 10.1109/OJPEL.2025.3639205.

Repository evidence: Constrained_BO/results/GP_BO_vs_random_search_RW9.md; RW9 and RW9_random constrained_bo_results_n_calls_40.json and n_calls_80.json; outputs/finetune_two_stage_RW10-RW12/finetune_percent_summary.json.